# 目录

目录	4

Abstract	7

第一章 绪论	1

第一节 碳量子点概述	1

第二节 碳点的合成方法	2

第三节 碳点的表面功能化策略	3

一、 表面官能团修饰	3

二、 杂原子掺杂	4

三、 复合结构构建	4

第四节 碳量子点用于光催化产过氧化氢	5

一、 光催化产过氧化氢的基本原理	5

二、 常见光催化剂及改性策略	6

三、 碳点用于光催化产H2O2	7

第五节 碳点负载单原子降解污染物	8

一、 碳量子点直接催化作用及局限性	8

二、 碳量子点性能的提升策略	9

三、 碳点负载单原子电活化PMS降解污染物	11

第六节 研究内容及意义	13

一、 研究意义	13

二、 研究内容	14

三、 技术路线	15

第二章 功能化碳量子点光催化产过氧化氢研究	16

第一节 引言	16

第二节 实验材料与方法	18

一、 实验材料与仪器	18

二、 实验方法	19

第三节 结果与讨论	22

一、 碳量子点的形貌与结构	22

二、 碳量子点光催化产H2O2性能	26

三、 ORR活性位点的识别	29

四、 碳量子点高效产H2O2机理分析	32

第四节 本章小结	37

第三章 碳点负载单原子催化降解水中双酚A的研究	39

第一节 引言	39

第二节 实验材料与方法	41

一、 实验材料与仪器	41

二、 实验方法	41

第三节 结果与讨论	43

一、 单原子催化剂的结构表征	43

二、 单原子催化剂的电催化性能	46

三、 碳点促进单原子催化剂活化PMS的机理探究	48

第四节 本章小结	50

第四章 结论与展望	52

第一节 主要结论	52

第二节 建议与展望	53

参考文献	54

致谢	67

个人简历	68

在学期间发表的学术论文与研究成果	69

摘要

碳量子点(CQDs)凭借其可调的电子结构、优良的导电性和易耦合特性，在环境与能源催化领域展现出广阔的应用前景。然而，CQDs受限于活性位点匮乏、界面电荷转移能力不足以及反应路径单一等瓶颈，难以满足复杂催化反应的需求。针对上述挑战，本研究从CQDs的性能提升策略入手，分别采用有机分子接枝改性与单原子负载策略，构筑了两种高性能CQDs基复合材料，系统探究了其在光催化合成过氧化氢(H2O2)与电活化过一硫酸盐(PMS)降解双酚A(BPA)中的催化性能与机理，为提升CQDs基材料在复杂催化体系中的活性提供了新的设计思路，也为清洁能源合成与难降解污染物治理领域的高效催化剂开发奠定了理论基础。主要的研究内容及结果如下：

（1）为解决二电子氧还原反应中质子供体不足、动力学缓慢等问题，本研究通过席夫碱反应在CQDs表面接枝苯甲酰肼，成功构建了具有C=N-NH-C=O结构的集成催化微环境，该结构实现了对反应中间体的协同调控：C=O基团作为氧分子的特异性吸附位点，能够将氧的吸附构型转变为有利于O=O键活化的Pauling型吸附；而相邻的-NH-单元则充当质子供体，有效降低了PCET过程的能垒。得益于该结构，在无外加质子供体及无需额外曝气的温和条件下，苯甲酰肼改性CQDs(BD-CQDs)的H2O2产率达到1562 μmol g-1 h-1，为原始CQDs的3倍，且选择性高达92.5%，显著优于目前已报道的多数碳量子点光催化剂。

（2）本研究以碳氮化合物为基底，通过热解法制备了铁单原子催化剂(Fe/CQDs-SA)。CQDs的引入促进了Fe-O结构的形成，优化了铁原子的构型，显著抑制了金属原子的团聚。同时，CQDs增加了材料缺陷和电化学活性面积，加速了电子转移。电化学测试表明，在电流密度为40 mA cm⁻²的条件下，Fe/CQDs-SA可在250秒内实现对BPA 99.94%的高效去除，且在共存离子干扰及多次循环使用后仍保持优异稳定性。机理研究进一步揭示，该体系中不仅存在由PMS活化产生的硫酸根自由基(·SO42-)和羟基自由基(·OH)，CQDs边缘缺陷还能高效活化溶解氧生成非自由基单线态氧(1O2)，构建了自由基与非自由基协同作用的降解机制，显著提升了催化剂的抗环境干扰能力和降解效率。

关键词：碳量子点；表面改性；单原子催化剂；光催化产过氧化氢；电活化过一硫酸盐

# Abstract

Carbon quantum dots (CQDs) have shown great promise in environmental and energy catalysis due to their tunable electronic structure, excellent electrical conductivity, and ease of functionalization. However, their application in complex catalytic reactions is hindered by limitations such as scarce active sites, inadequate interfacial charge transfer, and restricted reaction pathways. To address these challenges, this study explores two performance-enhancing strategies for CQDs: organic molecular grafting and single-atom loading. These approaches were employed to construct two types of high-performance CQDs-based composite materials, which were systematically investigated for their catalytic performance in the photocatalytic synthesis of hydrogen peroxide (H2O2) and the electro-activation of peroxymonosulfate (PMS) for bisphenol A (BPA) degradation. Furthermore, the structure–activity relationships and underlying reaction mechanisms were thoroughly elucidated. The main research contents and findings are as follows:

(1) To overcome issues such as insufficient proton donors and sluggish kinetics in the two-electron oxygen reduction reaction, benzoyl hydrazine was grafted onto the surface of CQDs via a Schiff base reaction, constructing an integrated catalytic microenvironment featuring a C=N-NH-C=O structure. Experimental and theoretical analyses reveal that this structure enables synergistic regulation of reaction intermediates: the C=O group serves as a specific adsorption site for oxygen molecules, facilitating a Pauling-type adsorption configuration conducive to O=O bond activation, while the adjacent -NH- unit functions as a proton donator, effectively lowering the energy barrier of the proton-coupled electron transfer (PCET) process. Benefiting from this structure, under mild conditions without external proton donors or additional aeration, the benzoyl hydrazine-modified CQDs (BD-CQDs) achieved an H2O2 production rate of 1562 μmol g-1 h-1, nearly three times that of pristine CQDs, with a selectivity of 92.5%, significantly outperforming most reported carbon dot-based photocatalysts.

(2) Using nitrogen-doped carbon supported by carbon dots as a substrate, an iron single-atom catalyst (Fe/CQDs-SA) was synthesized via pyrolysis. The incorporation of CQDs facilitated the formation of Fe–O structures, optimized the configuration of iron atoms, and effectively suppressed metal aggregation. Additionally, CQDs increased the density of structural defects and the electrochemical active surface area, thereby enhancing electron transfer. Electrochemical tests showed that at a current density of 40 mA cm⁻², Fe/CQDs-SA achieved 99.94% removal efficiency of BPA within 250 seconds, maintaining excellent stability even under interference from coexisting ions and after multiple cycles. Mechanistic studies further revealed that in addition to sulfate radicals (·SO42-) and hydroxyl radicals (·OH) generated from PMS activation, the edge defects of CQDs efficiently activated dissolved oxygen to produce singlet oxygen (1O2), establishing a synergistic degradation mechanism involving both radical and non-radical pathways. This dual mechanism significantly enhanced the catalyst's environmental robustness and degradation efficiency.

Key Words: Carbon quantum dots; Surface modification; Single-atom catalysts; Photocatalytic hydrogen peroxide production; Electroactivation of peroxymonosulfate

\